Overview

Cassava starch bioplastics are produced using different processing methods (casting, extrusion, injection molding, compression molding) and combined with plasticizers and reinforcements to tune mechanical, water, thermal, and biodegradation behavior. The table below summarizes representative methodologies, materials, tests, key results, and limitations.

Cassava-Starch Bioplastics: Methods, Tests, Results, Limitations

| Method & Materials | Key Tests / Analyses | Selected Results | Main Limitations / Trade-offs | Citations |
| --- | --- | --- | --- | --- |
| Twin-screw extrusion + compression; cassava starch + glycerol (3:1) + 0.5–1.5% chitosan | Density, contact angle, water uptake, tensile, elongation, thermal, moisture, biodegradation, FTIR | Best at 0.5% chitosan: density 0.86 g/mL; contact angle 68.6°; water uptake 11%; tensile 2.02 MPa; elongation 54%; T ≈137.5 °C; fastest biodegradation (Kusumawati et al., 2025) | Tensile strength still low vs conventional plastics; increased stiffness with chitosan may limit flexibility; data short-term only (Kusumawati et al., 2025) | (Kusumawati et al., 2025) |
| Casting; cassava starch + gelatin + glycerol (cassava vs corn, rice starches) | Hardness, water absorption, biodegradation; FTIR, TGA, SEM | Cassava: hardness 57.2 N; water absorption 139.8%; 67% mass loss in 7 days (Jayalath et al., 2024) | Very high water uptake; rapid degradation may limit shelf life; no barrier gas data (Jayalath et al., 2024) | (Jayalath et al., 2024) |
| Casting; cassava peel starch + sorbitol (20–30%) + 0–6% MCC | Density, water uptake, tensile, elongation, FTIR | Tensile ↑ to 9–12 MPa at 6% MCC & 20% sorbitol; elongation, density, water uptake ↓ with MCC (Maulida et al., 2016) | Reinforcement improves strength but reduces flexibility and water absorption; no biodegradation data (Maulida et al., 2016) |  |
| Casting; cassava peel starch + OPEFB cellulose (0–50%) + glycerol (0–50%) | Tensile, Young’s modulus, water absorption, biodegradation (30 days) | Cellulose ↑ tensile 3.7→12.1 MPa and modulus 40→240 MPa; water absorption 37.3→23.3%; biodegradation 84.7→55.3% (more cellulose slows degradation). Glycerol had opposite effects (Ibe et al., 2025) | Trade-off between strength and biodegradation; high glycerol increases hydrophilicity and faster degradation (Ibe et al., 2025) |  |
| Injection molding; cassava starch + 30–40% glycerol or glycerol/water | DMA, tensile, water uptake, soluble matter, SEM, XRD; RH effects | 30% glycerol gave low water uptake and uniform structure; mixed glycerol–water plasticizer produced harder but RH-sensitive materials (González et al., 2023) | Strong sensitivity to relative humidity; no biodegradation tests reported (González et al., 2023) |  |
| Casting; cassava starch + 2.5–10% banana bunch cellulose + glycerol | Tensile, Young’s modulus, elongation, water vapor absorption, biodegradability | At 7.5% cellulose: tensile 6.72 MPa; modulus 172.5 MPa; elongation 4.1%; water vapor absorption 11.5%; biodegradability index 50.7% (Saputri et al., 2024) | Higher cellulose decreases flexibility; only moderate strength; biodegradation measured but limited detail on conditions (Saputri et al., 2024) |  |
| Casting; cassava starch (pulp or commercial) + glycerol 30% + varying chitosan | Density, thickness, moisture adsorption, solubility, biodegradability; visual/optical | Commercial starch films showed higher moisture adsorption, solubility, and biodegradability than hand-extracted starch (Dodino-Duarte et al., 2024) | More chitosan caused bubbles/opacity; focus on basic properties, no mechanical or barrier numbers reported (Dodino-Duarte et al., 2024) |  |
| Casting; cassava + chitosan blends in various ratios | Contact angle, tensile, compressive strength, water resistance, biodegradation | Contact angle improved up to 97.8°; tensile strength increased; fastest biodegradation in 9 days at cassava:chitosan 6:4 (Albar et al., 2024) | Rapid degradation (9 days) may be unsuitable for many packaging uses; long-term stability unreported (Albar et al., 2024) |  |
| Casting; cassava starch + onion peel powder + crude glycerol (RSM/CCD) | Tensile, elongation, soil-burial biodegradation (30 days) | Optimised films reached tailored combinations of tensile strength, elongation, and ~29–32% weight loss in 30 days (Torche et al., 2025) | Optimization limited to mechanics + biodegradability; barrier and thermal properties not optimised (Torche et al., 2025) |  |
| Casting; cassava waste starch + clove oil | Antimicrobial halo test, water vapor permeability, tensile, elongation | Antimicrobial halo ~11.9 mm; WVP 0.14 g·mm/m·h·kPa; tensile 0.17 MPa; elongation 32.9% (Wahyuningtiyas & Suryanto, 2017) | Very low tensile strength; no reported biodegradation data; only water vapor barrier measured (Wahyuningtiyas & Suryanto, 2017) |  |
| Compression molding; thermoplastic cassava starch + 10–60% lemongrass fibre | FTIR, TGA, SEM, tensile, flexural, moisture absorption, soil burial | Best at 50% fibre: maximum tensile and flexural modulus; improved thermal stability; biodegradation slowed vs neat starch (Santana et al., 2023) | Higher fibre slows biodegradation; moisture absorption still present; no permeability data (Santana et al., 2023) |  |
| Casting; modified cassava starch + 25–100% PVA + glycerol + citric acid | Tensile (ASTM D882), TGA | 25% PVA notably ↑ tensile strength; 100% PVA slightly ↑ elongation; 50% PVA ↑ decomposition temperature (better thermal stability) (Silveira et al., 2025) | Water sensitivity of starch not fully overcome; no biodegradation or barrier tests (Silveira et al., 2025) |  |
| Microwave + freeze-drying; cassava starch foams (dual-modified) | FTIR, TGA, XRD, SEM, ¹³C NMR, compression set, water absorption, density, aerobic compost biodegradation | Water absorption as low as 65.6–70.8%; density 124–245 kg/m³; >50% biodegradation in 15 days (Kamaruddin et al., 2022) | Focus on foams not films; mechanical data limited to compression; long-term durability unreported (Kamaruddin et al., 2022) |  |
| Extrusion + compression; cassava starch + glycerol (3:1) | Biodegradability by modified ASTM G21-70 (fungus), dip-hanging, soil burial; weight loss, visual changes | A. niger grew well (ASTM G21); 11.5% weight loss (dip-hanging, 10 days); 29.9% weight loss in soil burial, with cracks and darkening (Syamani et al., 2020) | Short (10-day) tests only; no mechanical or barrier data; lab-scale conditions (Syamani et al., 2020) |  |
| Blending + casting; chitosan + cassava peel starch (5–20 mL starch) | Water resistance, thickness, tensile, elongation, Young’s modulus, FTIR; soil & river biodegradation | At 5 mL starch: water resistance 45%; thickness 0.019 mm; tensile 49.93 MPa; Young’s modulus 1627 MPa; mass loss 63% (soil), 54% (river) (Santos et al., 2025) | High strength but very low elongation (3.1%); strong stiffness–flexibility trade-off; only mass-loss biodegradation metric (Santos et al., 2025) |  |

Figure 1: Methods, tests, results, and key limitations for cassava-starch bioplastics.

Summary

Across studies, common methods include solution casting, extrusion plus compression molding, and injection molding, combined with plasticizers (glycerol, sorbitol) and reinforcements (cellulose fibers, chitosan, PVA, plant extracts). Tests focus on mechanical properties, water behavior, thermal stability, microstructure, and biodegradation. Typical limitations are trade-offs between strength and flexibility, barrier and biodegradability, high water sensitivity, short biodegradation test periods, and lack of full property optimization in a single formulation.

These search results were found and analyzed using Consensus, an AI-powered search engine for research. Try it at https://consensus.app. © 2026 Consensus NLP, Inc. Personal, non-commercial use only; redistribution requires copyright holders’ consent.

References

, M., Siagian, M., & Tarigan, P. (2016). Production of Starch Based Bioplastic from Cassava Peel Reinforced with Microcrystalline Celllulose Avicel PH101 Using Sorbitol as Plasticizer. Journal of Physics: Conference Series, 710. https://doi.org/10.1088/1742-6596/710/1/012012

Albar, N., Anuar, S., Azmi, A., Soh, S., Bhubalan, K., Ibrahim, Y., Khalik, W., Abdullah, N., & Yahya, N. (2024). Chemical, Mechanical, and Wettability Properties of Bioplastic Material from Manihot esculenta Cassava–Chitosan Blends as Plastic Alternative. Starch - Stärke. https://doi.org/10.1002/star.202300278

Dodino-Duarte, I., Quiroz-Ortega, L., Arias-Benítez, J., & García-León, R. (2024). Development of biodegradable plastic films from cassava starch. DYNA. https://doi.org/10.15446/dyna.v91n233.112073

González, C., Castillo, E., Flores, S., Gerschenson, L., & Bengoechea, C. (2023). Effect of plasticizer composition on the properties of injection molded cassava starch-based bioplastics. Food Packaging and Shelf Life. https://doi.org/10.1016/j.fpsl.2023.101218

Ibe, M., Ngozi, V., Cynthia, O., & Wirnkor, V. (2025). Synthesis and Characterization of Starch-Based Bioplastics Derived from Cassava (Manihot esculenta) Peels and Oil Palm Empty Fruit Bunch (Elaeis guineensis). Green Chemistry Innovations. https://doi.org/10.64229/wa7g9q43

Jayalath, U., Samaraweera, H., & Samarasinghe, A. (2024). Development and Characterization of Gelatin-Starch Bioplastics: A Comparative Study of Cassava, Corn, and Rice-Based Alternatives. Sustainable Chemistry for the Environment. https://doi.org/10.1016/j.scenv.2024.100190

Kamaruddin, Z., Jumaidin, R., Ilyas, R., Selamat, M., Alamjuri, R., & Yusof, F. (2022). Biocomposite of Cassava Starch-Cymbopogan Citratus Fibre: Mechanical, Thermal and Biodegradation Properties. Polymers, 14. https://doi.org/10.3390/polym14030514

Kusumawati, R., , S., Abdullah, A., Nissa, R., Firdiana, B., Handayani, R., Munifah, I., Dewi, F., Basmal, J., & Wibowo, S. (2025). Physical Properties of Biodegradable Chitosan-Cassava Starch Based Bioplastic Film Mechanics. Science and Technology Indonesia. https://doi.org/10.26554/sti.2025.10.1.191-200

Santana, I., Félix, M., & Bengoechea, C. (2023). Sustainable Biocomposites Based on Invasive Rugulopteryx okamurae Seaweed and Cassava Starch. Sustainability. https://doi.org/10.3390/su16010076

Santos, J., Silva, C., Silva, B., Britto-Costa, P., Costa, C., Otubo, L., Carbonari, A., & Cabrera-Pasca, G. (2025). Enhancing Cassava Starch Bioplastics with Vismia guianensis Alcoholic Extract: Characterization with Potential Applications. Polymers, 17. https://doi.org/10.3390/polym17030419

Saputri, C., Julyatmojo, F., , H., Febrina, M., Mahardika, M., & Maulana, S. (2024). Characteristics of bioplastics prepared from cassava starch reinforced with banana bunch cellulose at various concentrations. IOP Conference Series: Earth and Environmental Science, 1309. https://doi.org/10.1088/1755-1315/1309/1/012006

Silveira, Y., Franca, A., & Oliveira, L. (2025). Cassava Waste Starch as a Source of Bioplastics: Development of a Polymeric Film with Antimicrobial Properties. Foods, 14. https://doi.org/10.3390/foods14010113

Syamani, F., Kusumaningrum, W., Akbar, F., , I., Widyaningrum, B., & Pramasari, D. (2020). Characteristics of bioplastic made from modified cassava starch with addition of polyvinyl alcohol. IOP Conference Series: Earth and Environmental Science, 591. https://doi.org/10.1088/1755-1315/591/1/012016

Torche, A., Toufik, C., Djeghim, F., Sanah, I., Arhab, R., D’Elia, M., & Rastrelli, L. (2025). Optimization of Cassava Starch/Onion Peel Powder-Based Bioplastics: Influence of Composition on Mechanical Properties and Biodegradability Using Central Composite Design. Foods, 14. https://doi.org/10.3390/foods14142414

Wahyuningtiyas, N., & Suryanto, H. (2017). Analysis of Biodegradation of Bioplastics Made of Cassava Starch. , 1, 24-31. https://doi.org/10.17977/um016v1i12017p024